SPECIFICATION FOR WET-CAST RETAINING WALL UNITS

PART 1: GENERAL

1.01	Description

A. Work shall consist of furnishing materials, labor, equipment and supervision to install a segmental retaining wall system in accordance with plans and specifications and in reasonably close conformity with the lines, grades, design and dimensions shown on plans or established by Owner or Owner’s Engineer.

1.02 	Reference Standards

A. Wet-Cast Retaining Wall Units

- ASTM C 94 – Standard Specification for Ready-Mixed Concrete

- ASTM C 1776/C 1776 M-17 – Standard Specification for Wet-Cast Precast Modular Retaining Wall Units

B. Geosynthetic Reinforcement

1. ASTM D 4595 – Standard Test Method for Tensile Properties of Geotextiles by the Wide-Width Strip Method

2. ASTM D 5262 – Standard Test Method for Evaluating the Unconfined Tension Creep and Creep Rupture Behavior of Geosynthetics

3. ASTM D 5321 – Standard Test Method for Determining the Shear Strength of Soil-Geosynthetic and Geosynthetic-Geosynthetic Interfaces by Direct Shear

4. ASTM D 5818 – Standard Practice for Exposure and Retrieval of Samples to Evaluate Installation Damage of Geosynthetics

5. ASTM D 6706 – Standard Test Method for Measuring Geosynthetic Pullout Resistance in Soil

C. Soils

1. ASTM D 698 – Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Standard Effort

2. ASTM D 2487 – Standard Practice for Classification of Soils for Engineering Purposes (Unified Soil Classification System)

3. ASTM D 422 – Standard Test Method for Particle-Size Analysis of Soils

4. ASTM D 4318 – Standard Test Methods for Liquid Limit, Plastic Limit and Plasticity Index of Soils

5. ASTM G 51 – Standard Test Method for Measuring pH of Soil for Use in Corrosion Testing

D. Drainage Pipe

1. ASTM F 758 – Standard Specification for Smooth-Wall Polyvinyl Chloride (PVC) Plastic Underdrain Systems for Highway, Airport and Similar Drainage

2. ASTM F 405 – Standard Specification for Corrugated Polyethylene (PE) Pipe and Fittings

E. Engineering Design

1. “NCMA Design Manual for Segmental Retaining Walls,” 3rd Edition, 2009.

F. Where specifications and reference documents conflict, the Wall Design Engineer shall make the final determination of applicable document.

1.03	Submittals

A. Materials Submittals: The Contractor shall submit manufacturers’ certifications two weeks prior to start of work stating that the wet-cast retaining wall units and geosynthetic reinforcement meet the requirements of Section 2 of this specification.

B. Design Submittal: The Contractor shall submit two sets of detailed design calculations and

final retaining wall plans for approval at least two weeks prior to the beginning of wall construction. All calculations and drawings shall be prepared and stamped by a professional Civil Engineer (P.E.) – (Wall Design Engineer) experienced in SRW design and licensed in the state where the wall is to be built.

1.04	Delivery, Storage and Handling

- Contractor shall check materials upon delivery to ensure that the specified type and grade of materials have been received and proper color and texture of wet-cast retaining wall units have been received.

B. Contractor shall store and handle materials in accordance with manufacturer’s recommendations and in a manner to prevent deterioration or damage due to moisture, temperature changes, contaminants, corrosion, breaking, chipping or other causes.

C. Contractor shall prevent excessive mud, wet concrete, epoxies and similar materials that may affix themselves from coming in contact with materials.

D. Contractor shall protect materials from damage; no damaged material shall be incorporated into the segmental wall.

E. Geosynthetic shall be protected from UV exposure and the protective covering on geosynthetic shall remain until immediately before installation and shall be stored at temperatures above -10 degrees F.

PART 2: MATERIALS

2.01 	Wet-Cast Retaining Wall Units

A.	Wet-cast blocks shall be wet-cast, Portland cement concrete blocks specifically designed for retaining wall applications. Wet-cast blocks approved for this project are:

1. VERSA-LOK Bronco® 18H units supplied by VERSA-LOK, 651-770-3166.

B.	Finish of wet-cast retaining wall units shall be formed to mimic cut and split natural stone.

C.	Wet-cast retaining wall units shall be 18” high by 48” wide by 24” deep.

D.	Wet-cast retaining wall units shall provide a minimum weight of 120 psf wall face area.

E.	Wet-cast retaining wall units shall be interlocked with alignment knobs and receiving slots designed with proper setback to provide a 3-degree cant from vertical.

F.	Wet-cast retaining wall units shall be sound and free of cracks or other defects that would interfere with the proper placing of the unit or significantly impair the strength or permanence of the structure. Dime-size bug holes on the block face may be patched.

G.	Concrete used to manufacture wet-cast retaining wall units shall be made with ready-mixed concrete in accordance with ASTM C 94 and have a minimum 28 days’ compressive strength of 3,000 psi.

H.	Exterior block dimensions shall be uniform and consistent. Maximum dimensional deviations shall be 0.5 inch or 2 percent, whichever is less, excluding architectural surfaces. Maximum depth (face to back) deviation including architectural surface shall be 0.5 inch.

2.02	Geosynthetic Reinforcement

A. 	Geosynthetic reinforcement shall consist of high-tenacity PET geogrids, HDPE geogrids, or geotextiles manufactured for soil reinforcement applications. The type, strength and placement of the geosynthetic reinforcement shall be determined by procedures outlined in this specification and the “NCMA Design Manual for Segmental Retaining Walls,” (3rd Edition, 2009), and materials shall be specified by the Wall Design Engineer in their final wall plans and specifications. The manufacturers/suppliers of the geosynthetic reinforcement shall have demonstrated construction of similar size and types of segmental retaining walls on previous projects.

The geosynthetic type must be approved one week prior to bid opening. Geosynthetic types currently approved for this project are:

VERSA-Grid® Geogrids

B. 	The type, strength and placement of the reinforcing geosynthetic shall be as determined by the Wall Design Engineer, as shown on the final, P.E.-sealed retaining wall plans.

2.03	Leveling Pad

A.	Material for leveling pad shall consist of compacted sand, gravel, or combination thereof (USCS soil types GP, GW, SP and SW) and shall be a minimum of 6 inches in depth. Lean concrete with a strength of 200-300 psi and 3 inches thick maximum may also be used as a leveling pad material. The leveling pad shall extend laterally at least a distance of 6 inches from the toe and heel of the lowermost SRW unit.

2.04	Drainage Aggregate

A.	Drainage aggregate shall be angular, clean stone or granular fill meeting the following gradation as determined in accordance with ASTM D 422.

Sieve Size		Percent Passing

1 inch			100

3/4 inch			75-100

No. 4			0-60

No. 40			0-50

No. 200			0-5

2.05	Drainage Pipe

A.	The drainage collection pipe shall be a perforated or slotted PVC, or corrugated HDPE pipe. The drainage pipe may be wrapped with a geotextile to function as a filter.

B. Drainage pipe shall be manufactured in accordance with ASTM F 405 or ASTM F 758.

2.06 	Reinforced Backfill Soil

A.	The reinforced soil material shall be free of debris. Unless otherwise noted on the final, P.E.-sealed retaining wall plans prepared by the Wall Design Engineer, the reinforced material shall consist of the inorganic USCS soil types GP, GW, SW, SP and SM, meeting the following gradation, as determined in accordance with ASTM D 422:

Sieve Size		Percent Passing

1 inch			100

No. 4			20-100

No. 40			0-60

No. 200			0-35

B.	The maximum particle size of poorly-graded gravels (GP, no fines) should not exceed 3/4 inch unless expressly approved by the Wall Design Engineer and the long-term design strength (LTDS) of the geosynthetic is reduced to account for additional installation damage from particles larger than this maximum.

C. The plasticity of the fine fraction shall be less than 20.

D. The pH of the backfill material shall be between 3 and 9 when tested in accordance with ASTM G 51.

PART 3: DESIGN PARAMETERS

3.01	Soil

A.	The following soil parameters, as determined by the Owner's Geotechnical Engineer, shall be used for the preparation of the final design:

Unit Weight		Internal Friction 		Cohesion (c)

() (pcf)		Angle () (degrees)		(psf)

Reinforced Fill		________	____________		0

Retained Soil		________	____________		0

Foundation Soil		________	____________		__________

(If internal friction angles are not available for the above section, the specifier can provide the USCS soil type classification for the reinforced, retained and foundation soils and/or attach the geotechnical investigation report for this project.)

B.	Should the actual soil conditions observed during construction differ from those assumed for the design, the design shall be reviewed by the Wall Design Engineer at the Owner's Geotechnical Engineer's direction.

3.02	Design

A.	The design analysis for the final, P.E.-sealed retaining wall plans prepared by the Wall Design Engineer shall consider the external stability against sliding and overturning, internal stability and facial stability of the reinforced soil mass, and shall be in accordance with acceptable engineering practices and these specifications. The internal and external stability analysis shall be performed in accordance with the “NCMA Design Manual for Segmental Retaining Walls,” (3rd Edition, 2009), using the recommended minimum factors of safety in this manual.

B.	External stability analysis for bearing capacity, global stability, and total and differential settlement shall be the responsibility of the Owner and the Owner's Geotechnical Engineer. The Geotechnical Engineer shall perform bearing capacity, settlement estimates, and global stability analysis based on the final wall design provided by the Wall Design Engineer and coordinate any required changes with the Wall Design Engineer.

C.	While vertical spacing between geogrid layers may vary, it shall not exceed 2.5 feet maximum in the wall design.

D.	The geosynthetic placement in the wall design shall have 100% continuous coverage parallel to the wall face. Gapping between horizontally adjacent layers of geosynthetic (partial coverage) will not be allowed.

PART 4: CONSTRUCTION

4.01	Inspection

A.	The Owner or Owner's Representative is responsible for verifying that the Contractor meets all the requirements of the specification. This includes all submittals for materials and design, qualifications and proper installation of wall system.

B.	Contractor's field construction supervisor shall have demonstrated experience and be qualified to direct all work at the site.

4.02	Excavation

A.	Contractor shall excavate to the lines and grades shown on the project grading plans. Contractor shall take precautions to minimize over-excavation. Over-excavation shall be filled with compacted infill material, or as directed by the Engineer/Architect, at the Contractor's expense.

B.	Contractor shall verify location of existing structures and utilities prior to excavation. Contractor shall ensure all surrounding structures are protected from the effects of wall excavation. Excavation support, if required, is the responsibility of the Contractor.

4.03	Foundation Preparation

A.	Following the excavation, the foundation soil shall be examined by the Owner's Engineer to assure actual foundation soil strength meets or exceeds the assumed design bearing strength. Soils not meeting the required strength shall be removed and replaced with infill soils, as directed by the Owner's Geotechnical Engineer.

B.	Foundation soil shall be proof-rolled and compacted to 95% standard Proctor density and inspected by the Owner's Geotechnical Engineer prior to placement of leveling pad materials.

4.04	Leveling Pad Construction

A.	Leveling pad shall be placed as shown on the final, P.E.-sealed retaining wall plans with a minimum thickness of 6 inches. The leveling pad shall extend laterally at least a distance of 6 inches from the toe and heel of the lowermost wet-cast retaining wall unit.

B.	Granular leveling-pad material shall be compacted to provide a firm, level bearing surface on which to place the first course of units. Well-graded sand can be used to smooth the top 1/4 inch to 1/2 inch of the leveling pad. Compaction will be with mechanical plate compactors to achieve 95% of maximum standard Proctor density (ASTM D 698).

4.05	Wet-Cast Block Installation

A.	All wet-cast blocks shall be installed at the proper elevation and orientation as shown on the wall profiles and details on the construction plans or as directed by the Engineer. The wet-cast block units shall be installed in general accordance with the manufacturer's recommendations. The specifications and drawings shall govern in any conflict between the two requirements.

B.	The first course of wet-cast blocks shall be placed on the leveling pad. The units shall be leveled side-to-side, front-to-rear and with adjacent units, and aligned to ensure intimate contact with the leveling pad. The first course is the most important to ensure accurate and acceptable results. No gaps shall be left between the front of adjacent units. Alignment may be done by means of a stringline or offset from base line to the back of the units.

C.	Place and compact angular, clean drainage aggregate (3/4" to 1") in voids between blocks. Clean all excess debris from top of units and install next course.

D.	Place next course of blocks so that the receiving slot at the bottom of the upper block rests on top of the alignment knobs on the lower blocks. Push units forward to remove any looseness in the unit-to-unit connection and then check alignment. Check level and alignment of the units.

E.	Layout and installation of curves and corners shall be in accordance with the plan details or in general accordance with wet-cast retaining wall unit’s manufacturer's installation guidelines.

F.	Repeat procedures to extent of wall height.

G.	The wall face cant shall not differ more than + 2 degrees from that specified.

4.06	Geosynthetic Reinforcement Placement

A.	All geosynthetic reinforcement shall be installed at the proper elevation and orientation as shown on the final P.E.-sealed retaining wall plan profiles and details, or as directed by the Wall Design Engineer.

B.	At the elevations shown on the final plans—after the units, drainage material and backfill have been placed to this elevation—the geosynthetic reinforcement shall be laid horizontally on compacted infill and on top of the concrete wet-cast retaining wall unit. Extend the geosynthetic reinforcement to within 1 inch of the front of the sculpted face of the unit below. The geosynthetic reinforcement should be as far forward as possible without revealing itself on the wall face. Embedment of the geosynthetic in the wet-cast retaining wall units shall be consistent with the wet-cast retaining wall unit’s manufacturer’s recommendations. Correct orientation of the geosynthetic reinforcement shall be verified by the Contractor to be in accordance with the geosynthetic manufacturer’s recommendations. The highest-strength direction of the geosynthetic must be perpendicular to the wall face.

C.	Geosynthetic reinforcement layers shall be one continuous piece for their entire embedment length. Splicing of the geosynthetic in the design-strength direction (perpendicular to the wall face) shall not be permitted. Along the length of the wall, horizontally adjacent sections of geosynthetic reinforcement shall be butted in a manner to assure 100% coverage parallel to the wall face.

D.	Tracked construction equipment shall not be operated directly on the geosynthetic reinforcement. A minimum of 6 inches of backfill is required prior to operation of tracked vehicles over the geosynthetic. Turning should be kept to a minimum. Rubber-tired equipment may pass over the geosynthetic reinforcement at slow speeds (less than 5 mph).

E.	The geosynthetic reinforcement shall be free of wrinkles prior to placement of soil fill. Nominal tension shall be applied to the geosynthetic reinforcement and secured in place with staples, stakes or by hand tensioning until reinforcement is covered by 6 inches of fill.

4.07	Drainage Aggregate and Drainage Material Placement

A.	Drainage aggregate shall be installed to the line, grades and sections shown on the final P.E.-sealed retaining wall plans. Drainage aggregate shall be placed to the minimum thickness shown on the construction plans between and behind units (a minimum of 1 cubic foot for each exposed square foot of wall face unless otherwise noted on the final wall plans).

B.	Drainage collection pipes shall be installed to maintain gravity flow of water outside the reinforced-soil zone. The drainage collection pipe shall be installed at the locations shown on the final construction drawings. The drainage collection pipe shall daylight into a storm sewer or along a slope, at an elevation below the lowest point of the pipe within the aggregate drain. Drainage laterals shall be spaced at a maximum 50-foot spacing along the wall face.

4.08 	Backfill Placement

A.	The reinforced backfill shall be placed as shown in the final wall plans in the maximum compacted lift thickness of 8 inches and shall be compacted to a minimum of 95% of standard Proctor density (ASTM D 698) at a moisture content within -1% point to +3% point of optimum. The backfill shall be placed and spread in such a manner as to eliminate wrinkles or movement of the geosynthetic reinforcement and the SRW units.

B.	Only hand-operated compaction equipment shall be allowed within 3 feet of the back of the wall units. Compaction within the 3 feet behind the wall units shall be achieved by at least three passes of a lightweight mechanical tamper, plate or roller.

C.	At the end of each day's operation, the Contractor shall slope the last level of backfill away from the wall facing and reinforced backfill to direct water runoff away from the wall face.

D.	At completion of wall construction, backfill shall be placed level with the final top of wall elevation. If final grading, paving, landscaping and/or storm drainage installation adjacent to the wall is not placed immediately after wall completion, temporary grading and drainage shall be provided to ensure water runoff is not directed at the wall nor allowed to collect or pond behind the wall until final construction adjacent to the wall is completed.

4.09	Cap Units

A.	Finish top of wall by placing Bronco 18H Tapered Top Units or Universal Flat Cap Units as shown on the wall profiles and details on the construction plans or as directed by the Engineer.

B. 	Finish top of wall area behind cap units by placing and compacting impervious and backfill soil as shown on construction plans.

4.10	Construction Adjacent to Completed Wall

A.	The Owner or Owner's Representative is responsible for ensuring that construction by others adjacent to the wall does not disturb the wall or place temporary construction loads on the wall that exceed design loads, including loads such as water pressure, temporary grades, or equipment loading. Heavy paving or grading equipment shall be kept a minimum of 3 feet behind the back of the wall face. Equipment with wheel loads in excess of 150 psf live load shall not be operated within 10 feet of the face of the retaining wall during construction adjacent to the wall. Care should be taken by the General Contractor to ensure water runoff is directed away from the wall structure until final grading and surface drainage collection systems are completed.

END OF SECTION